# Lecture 20 Flexible Pavement Design

# A flexible road is composed of successive layers of weaker materials.  For an asphalt pavement this is a layer of asphalt followed by layers of base and sub base over the sub grade soils.   An example is shown in Typical Section.

Flexible pavement design is based on the concept that stress developed by the surface load is dissipated with depth and it is necessary to provide material that have adequate strength to resist the stress provided by the load. This usually results in a layered system with progressively weaker materials.

Since there are so many types of vehicles with different loads, axle configuration, and tire combination, it is standard practice to convert all loading to a standard loading using load factors.

Load factors were developed from the Ottawa road test completed in the late 1950's and are given in Table 20.3 (partial Table). There are other ways of developing load factors such as using load or fatigue relationships.  For a load factor directly proportional to an 18 kip load the factor would be

The Ottawa Road test used a different approach to obtain the load factors.  In this case the load factors were determined from the ratio of repeated loads to cause an equal increment of reduction in Pavement Serviceability Index (PSI). It looks like the following:

To convert traffic to ESAL (Equivalent single axle loads) use the following equation

ESALx = No axle loads (load x) X load factor(load x) X 365 X Growth factor

Where the load factor is from table 20.3 or is approximated by the equations.

# English weights

Using the approximation, at 10 kips the single axle value is 0.095 compared to 0.0877 from Table 20.3 and for tandem axle is .0075 compared to 0.00688 in the table

The Growth factor reflects the annual growth of traffic and is calculated as

n is the number of years and r is the annual growth rate.

Typical example using the axle weight and distribution from the AASHTO road test is:

It is possible to calculate truck factors for 2,3 or more axles by the same technique.  For example the following:

# 2-axle Truck factor = (.57*365)/150 = .57ESAL/year for each

2 axle truck(note the units)

3-axle truck factor = (9.5+20.1+21.05+69.98)*365/(25+10+5+50)

# =985ESAL/year for each 3 axle truck

5-axle truck Factor = (15.91+17.70+84.32+42.65)*365/(30+10+20+5)

# = 902ESAL/year for each 5 axle truck

The overall truck factor is

# Truck factor = (282.95-0.36)*365/260

= 396.71ESAL/year for each truck

# Considering all traffic

Traffic factor = 282.95*365/1260

# = 81.97ESAL/year for each vehicle per day

A more general equation for calculating ESAL is

# AADT = Annual Average Daily Traffic

Fd = directional distribution

# Gi = growth factor

TFi = Truck factor for axle number i.

PI = Percent of trucks with axle number i.

A Calculator for ESAL determination is available at

Calculator for ESAL